## Slide 1: SENKO-FLOW

## Slide 2: Flow of SENKO(wafer stock~chip stock)
①Wafer Stock
②Banchi Cleaving
③Banchi Anneal
Select a designated Banchi
④Bar Cleaving
⑤Bar Stack
⑥Coating
⑦Bar Unstack
⑧Chip Cleaving
Select the specified number of bars
⑨Chip Tester
⑩Chip output
⑪Chip Stock
SEM
※Specified 1 bar

## Slide 3: Flow of SENKO(After chip stock)
⑫LD D/B
⑬Stem mounted
⑭W/B（Wire Bonding)
⑮DC Sorting-１
⑰Aging
⑱DC Sorting-3
⑲Wire removal
⑳AC
㉑Visual inspection
㉒Macro test
⑯Purge

## Slide 4: Flow of SENKO(After Macro test)
Macro test passed
㉓W/B remove
㉔W/B
㉕IV Curve 0V
㉗IV Curve 100V
㉘ESD test ±300V
㉙ IV Curve 300V
㉚ESD Macro
㉖ESD test ±100V
Finish
※There are separate test items for the direct change process.

## Slide 5: Advance evaluation of major varieties Construction start banchi and number of construction starts
Variety | Use banchi number | Number of bars | Number of chips required for assembly
B5(3inch) | Ah,Bf,Cf,Da,Dh | 3 bars each | 10 Chips each(total50 chips)
B8 | Ah,Bf,Cf,Da,Dh | 3 bars each | 10 Chips each(total50 chips)
B5(4inch) | Ag,As,Bc,Bj,Cj,Ck,Da,Ds | 3 bars each | Da=8 chips others are 6 chips each(total50 chips)
E1 | Ah,Bf,Cf,Da,Dh | 3 bars each | 10 Chips each(total50 chips)
A6(4inch) | Aa,Ad,Af,Bf,Cf,Da,Dd,Df | 3 bars each | Aa=7 chips,Da=7 chips others are 6 chips each(total50 chips)
Currently, all bars are mounted on one ring

## Slide 6
B5(3inch)&E1
a b c d e f g h I j k l n m p q
Tested products
50 pcs
All bars may be installed
Each banchi requires a good product of 20chip or more.
a
h
q
q
h
a
or

## Slide 7
B5(4inch)
A6(4inch)

## Slide 8: Thank you